## Slide 1: Superconducting Nanoelectronics with Perovskite Oxides
By Sushant Padhye
Research Advisors: Dr. Evgeny Mikheev,
Dr. Marc Cahay
Physics: Design and fabrication, Electrical device testing, and Python programming to communicate with instruments
ECE: Cleanroom Certification, Device Simulation

## Slide 2: Big Picture
* David Schuster PhD thesis, “Circuit Quantum Electrodynamics”, 2007
https://rsl.yale.edu/sites/default/files/files/RSL_Theses/SchusterThesis.pdf
Side-view
Top-view
A
A
• Patterned Nb -> Resonator Meander for Qubit’s Read-out
• Al junctions -> Qubit
A: Resonators (Transmission Geometry)

## Slide 3: Big Picture
Resonators
Josephson Junction
Capacitor (Nb)
IBM’s 5 Qubit Processor
Currently used:
Silicon, Sapphire -> Insulating Substrates
Nb, Al -> Superconductors
New Material:
SrTiO3 -> Can be both insulator and superconductor

## Slide 4: SrTiO3 Crystal Chips
First CAD design
First device attempt
1: Hall bars
2: Contact resistance test structure (“TLM”)
3: Planar capacitor
1
2
3
1
1
1

## Slide 5: SrTiO3 Crystal Chips
I-V Curves for 2 terminal measurements
Zoomed-in view of the Hall Bar
GND
SRC

## Slide 6: Al Thin Film on SrTiO3
Testing stability over time
Unpatterned “witness” chip
No meaningful change over several weeks

## Slide 7
Resonators (Chip 3):
1
1: 6 hanger geometry resonators
2:
A: Large Hanger
B: 2 transmission C: 2 reflection resonators
2
A
B
C
Nb Thin Film Chips (On SrTiO3)

## Slide 8
Chip 2
Sheet resistance data from Hall Bars:
Nb Thin Film Chips (On Sapphire)

## Slide 9
* Y. Ivry, C-S. Kim et al, “Universal scaling of the critical temperature for thin films near the superconducting-to-insulating transition”. Phys. Rev. B, vol. 90, issue. 21, p 214515, Dec. 2014. (Also see Supplemental Material) https://journals.aps.org/prb/abstract/10.1103/PhysRevB.90.214515
Devised a model :
Predict
Critical temperature (Tc)
Using
Sheet resistance at room temperature (Rs)
Film thickness (d)
Nb Thin Film Chips

## Slide 10
Chip 3
SRC
GND
Quality Factor ≈ 3000 at optimal frequency (1-10 kHz)
IDC model calculation predicted ≈ 8 pF at SrTiO3 ’s room temperature dielectric constant (350)
* Bareesha R S et al, “Design and Optimization of Interdigital Capacitor”, 2018
https://ijret.org/volumes/2016v05/i33/IJRET20160533016.pdf
Capacitance data from IDC:
Nb Thin Film Chips (On SrTiO3)

## Slide 11
Things I learned:
Design, Fabrication and Testing of Devices
Automating pattern designs with code
Device Simulation (Ongoing)
Lab Setup
Questions?
Conclusion